### G20 Carpentry/Timber Framing/First Fixing

950 CELLULAR PVC FASCIA/BARGES/SOFFITS

Material:   Cellular PVC (PVC-ue)

Material Specification: To BS7619:1993:Type1

Manufacturer: Swish Building Products, Tamworth, Staffordshire, B79 7TF

Manufacturer accreditation:

- ISO 9001/2

- Class 1 Surface spread of flame to BS476 :Part 7 : 1987

# FASCIA

Profile:(1)    C286 Jumbo Board (175 x 20mm)

Finish/Colour:   White

Support timber:   Fix to rafter ends

Fixings:(2) C073 65mm A4 S/S Capped Screws

Fixing centres: 600mm maximum

Joints: C153 Concealed Fix Jumbo joints

# BARGEBOARD

Profile: (1)  C136 Cappair (163mm)

Finish/Colour:   White

Support timber:   Existing timber bargeboard

Fixings: (2)   C082 50mm Trimtop S/S nails

Fixing centres:   600mm maximum

Box end details: (5)    As Fig 29, Page 21 Swish Specification Guide

Joints:    C235 face fixed joint covers

FASCIA SOFFITS

Profile : (3)   C308 Polo Board (300mm)

Finish/Colour:   White

Fixings : (2) C081 40mm Trimtop A4 S/S nails

Fixing Centres :   200mm max centres across width and 600mm max along length.

Joints:    C041 Joint Trim.

BARGEBOARD SOFFITS

Profile: (3)    C246 GeePee Board (300mm)

Finish/Colour:    White

Fixings: (2)    C081 40mm Trimtop A4 S/S nails

Fixing Centres: 200mm max certres across width and 600mm max along length

Joints: C041 Joint Trim

## OVER-FASCIA VENTILATION/EAVES

PROTECTION

(4)   C502 Jumbotec & Eaves Ventilator Trays along full length of eaves

Fixings: (2)  Galvanised clout nails

Fixing centres:    200mm maximum

Corners:    C403 Sealing Tape as necessary

Sealing:   C403 Sealing Tape as necessary

Fixing procedures as per Swish Roofline Design and Specification Guide  A227

Notes :

(1)   Replacement, load bearing profiles: Square Jumbo, Bullnose Jumbo or Ogee Jumbo.

Refurbishment overcapping profiles: Cappit or Cappair.

(2)   Specify A4 Marine Grade stainless steel nails or screws.

(3)   Flat Boards: Gee Pee, Gee Pee with appropriate strip ventilators, Polo (vented flat board). Cladding as Soffit: Tee Gee, Open V, or Polo (vented) versions of these.

(4)  Eaves Protection: Jumbotec (without ventilator). Vented Eaves Protector C404.    Eaves Ventilators only: C504 & C505

(5) Boxend detail drawings may be found on pages 15/16 of the Swish Design & Specification Guide A227.  They are also printable from the Swish website in Technical Centre> Installation Guidance> Box Ends.

Please quote Swish References in all cases.