## H20 Rigid Sheet Cladding

### Type(s) of cladding system

150 CELLULAR PVC BOARD CLADDING

MATERIAL

Material:  Cellular PVC (PVC-ue)

Material Specification: To BS 7619 1993:Type1, BBA Certified

Colour stability Delta PI<15 in ACT test Delta L* less than –2 after 500 hrs in Suntest

Manufacturer: Swish Building Products, Tamworth, Staffordshire, B79 7TF

Manufacturer accreditation:  ISO9001/2

### PROFILES

Plank:  C001 100mm Shiplap, horizontal format

Finish/Colour: White

Class 1Y Surface spread of flame to BS476 :

Part 7 : 1987

ACCESSORIES

Starter:  Wall starter C028

Top:  Two-part universal trim C290/291

Vertical:  Two-part universal trim C290/291

#### Two-part corner trim C292/293

# Other:  N/A

SUPPORTS

Description: Treated timber battens & counterbattens

Dimensions :  25mm x 38mm

Placement: At the base and head, across intermediate areas, at reveals, openings and changes of direction.

Centres:  Maximum 600mm for all perimeter and intermediate battens.

### CLADDING FASTENINGS

Fixings: Swish 33mm A4 Stainless steel nails (C204)

Fixing location:  Secret fixing via groove in C001

Fixing centres:  600mm centres maximum

Running joints : Butt joints, using C042 joint covers over support timber

VENTILATION

Description: 25mm clear ventilated cavity

Ventilation profiles :  Swish angle ventilator C065

Breather membrane:  To BS 4016 : 1972

Sealing:  C077 Swish low modulus silicone

Insulation type:  N/A

Special features :  Vent top of cladding through eaves box

Fixing procedures as per Swish Cladding Design & Specification Guide.

Please quote Swish References in all cases.